Thwing samian

# THW 08- Context 266
- Fracture: granular
- Fabric: pink
- Inclusions: white (calcareous, different sizes, equally distributed); red; black spots
- Slip: orange-red
- Comments:
- Origin: Central Gaul – Lezoux

# T06- Context 47
- Fracture:
- Fabric: pink; denser than THW 08-266
- Inclusions: same range of inclusions as THW 08-266, but smaller sizes
- Slip: brown-reddish
- Comments: single external groove visible
- Origin: Central Gaul – Lezoux

# THWING 2007 Context 82 (500)
(A)
- Fracture: not granular
- Fabric: orange, dense
- Inclusions: yellowish calcareous, red, black (all small-sized), few mica
- Slip: red-brownish
- Comments: rim fragment (Dr 33?), shallow double internal groove just below rim
- Origin: Central Gaul – Lezoux

(B)
- Fracture: granular
- Fabric: red-orange
- Inclusions: white calcareous (unequal sizes), larger black spots, small mica plates
- Slip: brown-reddish
- Comments:
- Origin: Central Gaul – Lezoux

# THWING 2007 Context 82 (Z30)
- Fracture:
- Fabric: red, brick-colour
- Inclusions: lots of mica, quartz, elongated voids; no calcareous/white inclusions
- Slip:
- Comments:
- Origin: East Gaul?

# T05/ Context 17
- Fracture:
- Fabric: pink; denser than THW 08-266
- Inclusions: white calcareous, little else (some black spots, mica)
- Slip: red-brownish
- Comments: illegible stamp, Dr 18?
- Origin: Central Gaul – Lezoux